Mechanical Properties

Instructor/TA Notes

Answers to questions required in lab report, and typical results.

1.	The weight-percent composition of the four films are :  80% agar-20% glycerol; 60% agar-40% glycerol, 50% agar-50% glycerol, and 30% agar-30% starch-40% glycerol.

2.	Typical results are shown in the following table.

| wt % |  |  | t.s., Mpa (SD) | elong,% (SD) | elast.mod.,MPa (SD) |
| --- | --- | --- | --- | --- | --- |
| Agar | Starch | Glycerol |  |  |  |
| 80 | 0 | 20 | 13.7 (4.07) | 13 (7.3) | 300 (84.2) |
| 60 | 0 | 40 | 8.34 (2.22) | 37 (17) | 63.8 (3.75) |
| 50 | 0 | 50 | 5.02 (0.98) | 53 (8.2) | 23.4 (4.41) |
| 30 | 30 | 40 | 3.69 (0.45) | 51 (6.9) | 19.7 (4.85) |

3.	Glycerol decreases tensile strength and decreases elastic modulus but it increases elongation.

4.	Compared to the 60% agar - 40% glycerol film, replacing half the agar with starch weakens the film and lowers the modulus (it is less stiff), but increases elongation.