###### TA Notes for Polymers & Plastics Laboratory

The sample for the first pair/group doing this experiment may need to be prepared in advance.

Typical results:

| Wt % Agar | Starch | Glycerol | t.s., Mpa (SD) | elong., % (SD) | elast. mod., Mpa (SD) |
| --- | --- | --- | --- | --- | --- |
| 80 | 0 | 20 | 13.7 (4.07) | 13 (7.3) | 300 (84.2) |
| 60 | 0 | 40 | 8.34 (2.22) | 37 (17) | 63.8 (3.75) |
| 50 | 0 | 50 | 5.02 (0.98) | 53 (8.2) | 23.4 (4.41) |
| 30 | 30 | 40 | 3.69 (0.45) | 51 (6.9) | 19.7 (4.85) |

Glycerol decreases tensile strength and decreases elastic modulus but it increases elongation.